Technical data sheet

PLASTIC PRIMER

Product codes:	80151  0,5L

80120   1L

PRODUCT DESCRIPTION

APPLICATION

One-component colourless primer for application by brush or spray gun on car body parts made of plastic. In Car Refinish used as a primer coating and forming micro coating to obtain good adhesion topcoat to plastic.

Ready for use. Designed for application by brush or spray gun.

|  | Number of layers | 2 |  |
| --- | --- | --- | --- |
|  | Pressure | 2 - 2,5 bar |  |
|  | Nozzle | 1.3 - 1.4 mm |  |
|  | Flash off between layers: 20 min |  | Operating hardness: 30-40 min at 20°C |

After 30-40 min since applying the last layer of primer plastic, can be applied every type of topcoat.

| CONTENT OF VOLATILE ORGANIC COMPOUNDS |  |
| --- | --- |
| Maximum content of VOC in product | 810 g/l |
| VOC for category: II,B/e | 840 g/l |

STORAGE TIME AND CONDITIONS

Product complies standards of EU Directive 2004/42/CE/II,B/e(840)

Store in tightly closed containers, in a cool, dry place away from sources of fire and heat. Avoid exposure to sunlight. Expiration date: 12 months from date of manufacture - date on the top of container.

CLEANING EQUIPMENT

HEALTH AND SAFETY REGULATIONS

For cleaning equipment can be used acryl thinner or nitro thinner. It is recommended to use thinner for cleaning paint spray guns.

See Safety Data Sheet of the product.

SPECIFIC WEIGHT

About 0.9 g/cm3

OTHER INFORMATION

The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777