# Technical data sheet

# STONDER FIBERGLASS PUTTY PROFY

Glass fiber putty

Product code	77121  	1,8 kg

| PROPERTIES |  |  |
| --- | --- | --- |
| The STONDER FIBERGLASS PUTTY PROFY is reinforced with glass fiber. Thanks to elastic polyester resins and short glass fibers, the product is much elastic than the STONDER FIBERGLASS PUTTY putty while retaining high mechanical resistance. Its easy and soft treatment makes the product suitable even for large surfaces. STONDER FIBERGLASS PUTTY PROFY has a low volume shrinkage which makes it possible to repair large defects. The product has good adhesion to various substrates, including galvanised steel. |  |  |
| SUBSTRATES |  |  |
| polyester laminates | dry sand with P80-P120 and degrease again with the PLUS 780 silicone degreaser |  |
| steel | degrease, dry sand with P80 – P120, degrease again |  |
| galvanised steel | degrease, mat with an abrasive finishing pad and degrease again |  |
| aluminium | degrease, mat with an abrasive finishing pad and degrease again |  |
| two-component acrylic fillers | degrease, dry sand with P220 – P280, degrease again |  |
| old paint coatings | degrease, dry sand with P220 – P280, degrease again |  |
| CAUTION |  |  |
| Do not apply polyester putty directly on top wash primers or one-component acrylic and nitrocellulose products. The putty adheres to most types of galvanised steel used today. |  |  |
| MIXING RATIO |  |  |
| 2 100 | PUTTY HARDENER | Weight ratio |
|  |  | 100 g 2 g |
| APPLICATION LIFE FROM MIXING WITH THE HARDENER |  |  |
| 4 to 8 min at 20°C. |  |  |

| DRYING TIME |  |  |  |
| --- | --- | --- | --- |
| 20 to 30 min at 20°C. The time can be shortened by heating for 10 minutes at a maximum of 60°C. |  |  |  |
| COATABILITY |  |  |  |
| Polyester putties, spray polyester filler, acrylic primers, epoxy primers |  |  |  |
| APPLICATION CONDITIONS |  |  |  |
| The minimum application temperature is +10C |  |  |  |
| APPLICATION |  |  |  |
|  | Clean and sand the surface |  |  |
|  | Degrease the surface with silicone remover |  |  |
| 2 100 | Observe the required amount of hardener. Mix the components thoroughly until a uniform colour is obtained. Weight quantity of components: Add 100 g of FIBERGLASS PUTTY PROFY to 2 g of Hardener. Binding time: 4 to 8 minutes at 20C |  |  |
|  | Apply a layer of 5 mm max with a putty knife. |  |  |
|  | Wait for 20 to 30 minutes (at 20°C) |  |  |
|  | rough |  | finish |
|  | P80 – P120 |  | P120 – P240 |
| COLOUR |  |  |  |
| Green |  |  |  |
| CONTENT OF VOLATILE ORGANIC COMPOUNDS (VOC) |  |  |  |
| VOC II/B/b limit* = 250g/l |  | 90 g/l |  |
| *For ready to use mixture. |  |  |  |

| EQUIPMENT CLEANING |  |
| --- | --- |
| Acrylic thinner or NC solvent. |  |
| STORAGE CONDITIONS |  |
| Store in a cool dry room, away from sources of fire and heat. Avoid direct exposure to sunlight. |  |
| SHELF LIFE |  |
| FIBERGLASS PUTTY PROFY 1,8 kg | 24 months/20°C |
| SAFETY |  |
| See Safety Data Sheet. |  |
| NOTES |  |
| Intended for professional use only. |  |
| OTHER INFORMATION |  |
| The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final resultwas affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777 |  |