

Technical data sheet
STONDER FIBERGLASS PUTTY PROFY
Glass fiber putty
	
	Product code	77121  	1,8 kg


	PROPERTIES

	The STONDER FIBERGLASS PUTTY PROFY is reinforced with glass fiber. Thanks to elastic polyester resins and short glass fibers, the product is much elastic than the STONDER FIBERGLASS PUTTY putty while retaining high mechanical resistance. Its easy and soft treatment makes the product suitable even for large surfaces. STONDER FIBERGLASS PUTTY PROFY has a low volume shrinkage which makes it possible to repair large defects. The product has good adhesion to various substrates, including galvanised steel.

	SUBSTRATES

	polyester laminates
	dry sand with P80-P120 and degrease again with the PLUS 780 silicone degreaser

	steel
	degrease, dry sand with P80 – P120, degrease again

	galvanised steel
	degrease, mat with an abrasive finishing pad and degrease again

	aluminium
	degrease, mat with an abrasive finishing pad and degrease again

	two-component acrylic fillers
	degrease, dry sand with P220 – P280, degrease again

	old paint coatings
	degrease, dry sand with P220 – P280, degrease again

	CAUTION

	Do not apply polyester putty directly on top wash primers or one-component acrylic and nitrocellulose products.
The putty adheres to most types of galvanised steel used today.

	MIXING RATIO

	



2
100
	


PUTTY HARDENER
	Weight ratio

	
	
	100 g
2 g

	APPLICATION LIFE FROM MIXING WITH THE HARDENER

	4 to 8 min at 20°C.
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	DRYING TIME

	20 to 30 min at 20°C.
The time can be shortened by heating for 10 minutes at a maximum of 60°C.

	COATABILITY

	Polyester putties, spray polyester filler, acrylic primers, epoxy primers

	APPLICATION CONDITIONS

	The minimum application temperature is +10C

	APPLICATION

	

	

Clean and sand the surface



	

	

Degrease the surface with silicone remover



	

2
100
	Observe the required amount of hardener. Mix the components thoroughly until a uniform colour is obtained. Weight quantity of components: Add 100 g of FIBERGLASS PUTTY PROFY to 2 g of Hardener.
Binding time: 4 to 8 minutes at 20C

	

	
Apply a layer of 5 mm max with a putty knife.



	

	

Wait for 20 to 30 minutes (at 20°C)

	[image: ]

	rough
	finish

	
	P80 – P120
	P120 – P240

	COLOUR

	Green

	CONTENT OF VOLATILE ORGANIC COMPOUNDS (VOC)

	VOC II/B/b limit* = 250g/l
	90 g/l

	*For ready to use mixture.



	EQUIPMENT CLEANING

	Acrylic thinner or NC solvent.

	STORAGE CONDITIONS

	Store in a cool dry room, away from sources of fire and heat. Avoid direct exposure to sunlight.

	SHELF LIFE

	FIBERGLASS PUTTY PROFY 1,8 kg
	24 months/20°C

	SAFETY

	See Safety Data Sheet.

	NOTES

	Intended for professional use only.

	OTHER INFORMATION

	The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final resultwas affected by factors beyond our control.
   RAGS Ltd.,  Reg. No.: 40003133752, VAT number: LV40003133752
   Legal address: Durbes street 8, Rīga, LV-1007,  
   Actual address: Džūkstes street 1, Rīga, LV-1004
Tel. +371 67 808 780, +371 26 542 777


[bookmark: _GoBack]
image4.png




image5.png




image6.png




image7.png




image8.png




image9.png




image10.png




image1.png




image2.png




image3.png
STENDER |

Li:OR DROFESSIONAL'SJ





