


Technical data sheet
STONDER SPRAY PUTTY
Spray filler

	Product code		80702




	PROPERTIES

	SPRAY PUTTY spray filler – finishing filler applied by pneumatic spraying. Allows achieving a high fill ratio with a smooth surface, even on very large areas. The time to sand is approx. 2 hours at 20°C (and can be reduced by heating at a maximum of 60°C). The product is intended for machine sanding and manual sanding with fine abrasive papers.

	RELATED PRODUCTS

	CETOX 20 OE
	Hardener

	Spray filler thinner
	Thinner for polyester Spray Filler

	SUBSTRATES

	Old paint coatings
	degrease, dry sand with P220 – P280, degrease again.

	Polyester putties
	degrease, dry sand with P240, degrease again.

	Epoxy primers
	mat and degrease. If epoxy primers are used, apply the filler after a minimum of 4 hours from applying the epoxy primer.

	Steel surfaces
	degrease, dry sand with P80 – P120, degrease again.

	Aluminium surfaces
	degrease with silicone remover, mat with an abrasive finishing pad, degrease again.

	Plastics, except for PE, PP and PTFE
	degrease with silicone remover, mat with an abrasive finishing pad, degrease again.

	Two-component acrylic fillers
	degrease, dry sand with P220 – P280, degrease again.

	Note: Do not apply the spray filler directly on top wash primers or one-component acrylic and cellulose nitrate products.

	MIXING RATIO

	


	

SPRAY PUTTY
CETOX-20OE Spray filler thinner
	Volume ratio
	Weight ratio

	
	
	100 ml
6 to 7 ml
10 ml max
	100g
3.5 to 4.5g 6g max

	Add the thinner in the amount calculated for the mixture of SPRAY PUTTY with CETOX 20 OE.
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	CONTENT OF VOLATILE ORGANIC COMPOUNDS (VOC)

	VOC II/B/c limit* Actual VOC content
	540 g/l
300 g/l

	* For ready to use mixture acc. to EU Directive 2004/42/CE

	APPLICATION CONDITIONS

	It is recommended to apply the primer at a temperature above 10C and a humidity of no more than 80 %.

	APPLICATION

	

	Conventional gravity fed spray gun
CAUTION: Instructions of the equipment manufacturer must be followed.
	Nozzle
	Pressure
	Distance

	
	
	
2.2 – 3.0 mm
	
3 – 4 bar
	
15 – 20 cm

	

	Number of layers
	1 – 3

	
	Single wet layer thickness
	Approx. 100 µm

	
	The yield of the ready to use mixture for the given range of dry layer thickness
	
6.0 m2/l at 100 µm

	
	
Maximum total layer thickness
	
Approx. 300 µm

	

	
Mixture life at 20C
	
20 – 30 minutes
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Flash off time between layers
	
2 – 5 minutes

	DRYING TIMES

	

	20°C
	90 – 120 minutes

	
	60°C
	30 min

	CAUTION: The curing times apply to the temperatures of the individual elements.

	SANDING
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	rough
	finish

	
	P180 – P240
	P240 – P320

	COLOUR

	Grey



	COATABILITY

	[bookmark: _GoBack]Most commercial acrylic primers, epoxy primers, paint and varnishes.

	EQUIPMENT CLEANING

	Spray filler thinner or NC solvent.

	STORAGE CONDITIONS

	Store in a cool dry room, away from sources of fire and heat.     Avoid  direct exposure to sunlight.

	SHELF LIFE

	SPRAY PUTTY
	12 months/20°C

	Spray filler thinner
	24 months/20°C

	SAFETY

	See Safety Data Sheet.

	NOTES

	Intended for professional use only. The SPRAY filler must be used with the CETOX-20 OE hardeners and the Spray Filler   thinner only.
Using other systems (hardener, thinner) may result in insufficient curing of the filler and flaws in coating.

	OTHER INFORMATION

	The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control.
   RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752
   Legal address: Durbes street 8, Rīga, LV-1007, 
   Actual address: Džūkstes street 1, Rīga, LV-1004
Tel. +371 67 808 780, +371 26 542 777
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