# Technical data sheet

# STONDER SPRAY PUTTY

Spray filler

Product code		80702

| PROPERTIES |  |  |  |  |
| --- | --- | --- | --- | --- |
| SPRAY PUTTY spray filler – finishing filler applied by pneumatic spraying. Allows achieving a high fill ratio with a smooth surface, even on very large areas. The time to sand is approx. 2 hours at 20°C (and can be reduced by heating at a maximum of 60°C). The product is intended for machine sanding and manual sanding with fine abrasive papers. |  |  |  |  |
| RELATED PRODUCTS |  |  |  |  |
| CETOX 20 OE |  | Hardener |  |  |
| Spray filler thinner |  | Thinner for polyester Spray Filler |  |  |
| SUBSTRATES |  |  |  |  |
| Old paint coatings |  | degrease, dry sand with P220 – P280, degrease again. |  |  |
| Polyester putties |  | degrease, dry sand with P240, degrease again. |  |  |
| Epoxy primers |  | mat and degrease. If epoxy primers are used, apply the filler after a minimum of 4 hours from applying the epoxy primer. |  |  |
| Steel surfaces |  | degrease, dry sand with P80 – P120, degrease again. |  |  |
| Aluminium surfaces |  | degrease with silicone remover, mat with an abrasive finishing pad, degrease again. |  |  |
| Plastics, except for PE, PP and PTFE |  | degrease with silicone remover, mat with an abrasive finishing pad, degrease again. |  |  |
| Two-component acrylic fillers |  | degrease, dry sand with P220 – P280, degrease again. |  |  |
| Note: Do not apply the spray filler directly on top wash primers or one-component acrylic and cellulose nitrate products. |  |  |  |  |
| MIXING RATIO |  |  |  |  |
|  | SPRAY PUTTY CETOX-20OE Spray filler thinner |  | Volume ratio | Weight ratio |
|  |  |  | 100 ml 6 to 7 ml 10 ml max | 100g 3.5 to 4.5g 6g max |
| Add the thinner in the amount calculated for the mixture of SPRAY PUTTY with CETOX 20 OE. |  |  |  |  |

| CONTENT OF VOLATILE ORGANIC COMPOUNDS (VOC) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| VOC II/B/c limit* Actual VOC content |  |  |  | 540 g/l 300 g/l |  |  |  |
| * For ready to use mixture acc. to EU Directive 2004/42/CE |  |  |  |  |  |  |  |
| APPLICATION CONDITIONS |  |  |  |  |  |  |  |
| It is recommended to apply the primer at a temperature above 10C and a humidity of no more than 80 %. |  |  |  |  |  |  |  |
| APPLICATION |  |  |  |  |  |  |  |
|  |  |  | Conventional gravity fed spray gun CAUTION: Instructions of the equipment manufacturer must be followed. | Nozzle |  | Pressure | Distance |
|  |  |  |  | 2.2 – 3.0 mm |  | 3 – 4 bar | 15 – 20 cm |
|  |  |  | Number of layers | 1 – 3 |  |  |  |
|  |  |  | Single wet layer thickness | Approx. 100 µm |  |  |  |
|  |  |  | The yield of the ready to use mixture for the given range of dry layer thickness | 6.0 m2/l at 100 µm |  |  |  |
|  |  |  | Maximum total layer thickness | Approx. 300 µm |  |  |  |
|  |  |  | Mixture life at 20C | 20 – 30 minutes |  |  |  |
|  |  |  | Flash off time between layers | 2 – 5 minutes |  |  |  |
| DRYING TIMES |  |  |  |  |  |  |  |
|  |  | 20°C |  |  | 90 – 120 minutes |  |  |
|  |  | 60°C |  |  | 30 min |  |  |
| CAUTION: The curing times apply to the temperatures of the individual elements. |  |  |  |  |  |  |  |
| SANDING |  |  |  |  |  |  |  |
|  | rough |  |  |  | finish |  |  |
|  | P180 – P240 |  |  |  | P240 – P320 |  |  |
| COLOUR |  |  |  |  |  |  |  |
| Grey |  |  |  |  |  |  |  |

| COATABILITY |  |
| --- | --- |
| Most commercial acrylic primers, epoxy primers, paint and varnishes. |  |
| EQUIPMENT CLEANING |  |
| Spray filler thinner or NC solvent. |  |
| STORAGE CONDITIONS |  |
| Store in a cool dry room, away from sources of fire and heat. Avoid direct exposure to sunlight. |  |
| SHELF LIFE |  |
| SPRAY PUTTY | 12 months/20°C |
| Spray filler thinner | 24 months/20°C |
| SAFETY |  |
| See Safety Data Sheet. |  |
| NOTES |  |
| Intended for professional use only. The SPRAY filler must be used with the CETOX-20 OE hardeners and the Spray Filler thinner only. Using other systems (hardener, thinner) may result in insufficient curing of the filler and flaws in coating. |  |
| OTHER INFORMATION |  |
| The effectiveness of our systems results from laboratory research and many years of experience. The data contained herein meets the current knowledge about our products and their application potential. We ensure high quality, provided the user follows the instructions and the work is performed in accordance with good workmanship. It is necessary to do a test application of the product due to its potentially different reaction with different materials. We may not be held liable for defects if the final result was affected by factors beyond our control. RAGS Ltd., Reg. No.: 40003133752, VAT number: LV40003133752 Legal address: Durbes street 8, Rīga, LV-1007, Actual address: Džūkstes street 1, Rīga, LV-1004 Tel. +371 67 808 780, +371 26 542 777 |  |